|  | Product type | SMD power inductors |
| --- | --- | --- |
|  | Type | SER0805□□□ MAB |

- Product Description

  - 8.40×8.40mm Max. (L×W), 5.5mm Max. height.

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance Range:0.35～7.1μH (Standard type ); 0.5～10.0μH

(Low D.C.R type);0.2uH～4.0μH (High Power type).

  - Saturation Current range: 2.6～12.0A(Low D.C.R type); 3.8～18.4A

(Standard type ) ;7.2～32.0A (High Power type).

  - Temperature rise current 6.5～18.0A.

  - In addition to the standards versions shown here,

custom inductors are also available to meet your exact requirements.

- Feature& Application

  - Mn-Zn core used, Flat wire used.

  - Super high current Inductors, ideally used in portable computer CPU power supply.

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                         ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| SER0805 | 0.20~10 | 100KHz | 2.50~15 | 32~2.6 | 18.0~6.50 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 75% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | SMD power inductors |
| --- | --- | --- |
|  | Type | SER1030□□□ MAB |

- Product Description

  - 10.4×10.4mm Max. (L×W), 4.0mm Max. height.

  - Inductance range: 1.2～3.6uH.

  - Rated current range: 4.4～9.7A.

  - In addition to the reference versions of parameters shown here,

custom designs are available to meet your exact requirements.

- Feature& Application

  - Mn-Zn core used, Flat wire used.

  - Super high current Inductors, ideally used in portable computer CPU power supply.

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

Pad  Layout(mm)                            ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| SER1030 | 1.20 ~3.60 | 100KHz | 5.9~22.5 | 13.5~7.90 | 9.70~4.40 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 65% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | SMD power inductors |
| --- | --- | --- |
|  | Type | SER1040□□□MAB |

- Product Description

  - 10.4×10.4mm Max. (L×W), 4.5mm Max. height.

  - Both standard type and Low DCR type of SER1040 are available.

  - Inductance range: 0.22～2.50uH(SER1040 Standard type);0.36～4.3uH(SER1040 Low D.C.R type ).

  - Saturation Current range: 11.8～39.6A(SER1040 Standard type ) ;7.0～24.2A(SER1040 Low D.C.R type).

  - Temperature rise current 5.0～18.0A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements

- Feature& Application

  - Mn-Zn core used, Flat wire used.

  - Super high current Inductors, ideally used in portable computer CPU power supply.

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                          ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| SER1040 | 0.22 ~4.30 | 100KHz | 2.2~21.8 | 39.6~7.00 | 18.0~5.0 | 20℃ |

a、Saturation current: The DC current at which the inductance decreases to 65%

(for the inductance tolerance :±30%) or 75% (for the inductance tolerance:±20%)

of its nominal.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃(Ta＝20℃).

|  | Product type | SMD power inductors |
| --- | --- | --- |
|  | Type | SER1050□□□MAB |

- Product Description

  - 10.4×10.4mm Max. (L×W), 5.6mm Max. height.

  - Both standard type and Low DCR type of SER1050 are available.

  - Inductance Range:0.22～5.0uH (standard type );0.36～8.8μH(Low D.C.R type); 0.15～3.0μH (High Power type).

  - Saturation Current range: 8.4～40.0 A(Standard type ) ;4.8～24.0A(Low D.C.R type);12.6～55.0A (High Power type).

  - Temperature rise current 4.9～19.0A.

  - In addition to the standards versions shown here, custom inductors are also available tomeet your exact requirements.

- Feature& Application

  - Mn-Zn core used, Flat wire used.

  - Super high current Inductors, ideally used in portable computer CPU power supply.

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                            ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| SER1050 | 0.15 ~8.80 | 100KHz | 1.7~23.8 | 55.0~4.80 | 19.0~4.9 | 20℃ |

a、Saturation current: The DC current at which the inductance decreases to 65%

(for the inductance tolerance :±30%) or 75% (for the inductance tolerance:±20%)

of its nominal.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃(Ta＝20℃).

|  | Product type | SMD power inductors |
| --- | --- | --- |
|  | Type | SER1204□□□MAB |

- Product Description

  - 12.9×12.9mm Max. (L×W), 5.0mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance Range: 0.68～4.0μH (standard type );0.35～2.2μH (High Power type).

  - Saturation Current range: 8.8～20.8 A (Standard type ) ;16.2～38.4A

(High Power type).

  - Temperature rise current range 12.6～18.4A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Mn-Zn core used, Flat wire used.

  - Super high current Inductors, ideally used in portable computer CPU power supply.

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                           ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| SER1204 | 0.35~4.00 | 100KHz | 1.6~7.6 | 38.4~8.0 | 18.4~12.6 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 75% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | SMD power inductors |
| --- | --- | --- |
|  | Type | SER1205□□□MAB |

- Product Description

  - 12.9×12.9mm Max. (L×W), 5.6mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available

  - Inductance range : 0.68～10μH(Standard type );0.47～7.2μH(High Power type); 0.35～5.6μH (Ultra Power Type).

  - Saturation current range: 5.0～20.4A(Standard type ) ;

7.8～28.8A (High Power type); 9.5～35.0A (Ultra Power Type).

  - Temperature rise current range 7.6～19.5A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Mn-Zn core used, Flat wire used.

  - Super high current Inductors, ideally used in portable computer CPU power supply.

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                            ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| SER1205 | 0.35~10 | 100KHz | 1.5~13.5 | 35~5 | 19.5~7.6 | 20℃ |

a、 Saturation current: The DC current at which the inductance decreases to 65%

(for the inductance tolerance :±30%) or 75% (for the inductance tolerance:±20%)

of its nominal.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃(Ta＝20℃).

|  | Product type | SMD power inductors |
| --- | --- | --- |
|  | Type | SER1405□□□MAB |

- Product Description

  - 14.9×14.9mm Max. (L×W), 6.0mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance range : 0.68～6.1μH(Standard type );

0.56～5.0μH (High Power type).

  - Saturation Current range: 10.4～30.0A(Standard type ) ;

13.1～36.0A (High Power type).

  - Temperature rise current range 9.5～23.0A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Mn-Zn core used, Flat wire used.

  - Super high current Inductors, ideally used in portable computer CPU power supply.

  - Qualification to AEC-Q200

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                           ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| SER1405 | 0.56~6.10 | 100KHz | 1.70~10.8 | 36~10.4 | 23~9.5 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 75% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | SMD power inductors |
| --- | --- | --- |
|  | Type | SER1407□□□MAB |

- Product Description

  - 14.9×14.9mm Max. (L×W), 8.0mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance range: 0.5～12μH(Low D.C.R type); 0.4～9.5μH (standard type );

0.3～7.3μH(High Power type).

  - Saturation Current range: 8.0～39.6A(Low D.C.R type); 11.2～52.8A

(Standard type ) ;14.6～70A (High Power type).

  - Temperature rise current range 8.5～23.0A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Mn-Zn core used, Flat wire used.

  - Super high current Inductors, ideally used in portable computer CPU power supply.

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                          ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| SER1407 | 0.30~12 | 100KHz | 1.18~13.3 | 70~8.0 | 23~8.5 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 75% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | SMD power inductors |
| --- | --- | --- |
|  | Type | SER1810□□□MAB |

- Product Description

  - 22.4×19.2mm Max. (L×W), 11.0mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance Range : 5.6～33uH.

  - Saturation Current range: 5.5～12.0A .

  - Temperature rise current range 12.0～22.5A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Mn-Zn core used, Flat wire used.

  - Ideally used in PC and Game machine power supply

  - Operating temperature range: -40℃～+105℃(Including coil’s self temperature rise).

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                             ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| SER1810 | 2.2~33 | 100KHz | 1.50~9.0 | 15~5.5 | 22.5~12.0 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 75% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | SMD power inductors |
| --- | --- | --- |
|  | Type | SER2009□□□MAB |

- Product Description

  - 21.0×14.0mm Max. (L×W), 9.50mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance Range : 2.2～68uH.

  - Saturation Current range: 10～38.0A .

  - Temperature rise current range 8.0～30.0A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Mn-Zn core used, Flat wire used.

  - Ideally used in Power module DC-DC Converter

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                             ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| SER2009 | 2.2~68 | 100KHz | 1.00~20.0 | 38~10 | 8~30.0 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 80% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | SMD power inductors |
| --- | --- | --- |
|  | Type | SER2209□□□MAB |

- Product Description

  - 23.5×15.0mm Max. (L×W), 9.50mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance Range :1.0～100uH.

  - Saturation Current range: 12～45.0A .

  - Temperature rise current range 10～38.0A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Mn-Zn core used, Flat wire used.

  - Ideally used in Power module DC-DC Converter

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                             ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| SER2209 | 1.0~100 | 100KHz | 1.00~30.0 | 45.0~12.0 | 38.0~10 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 90% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | SMD power inductors |
| --- | --- | --- |
|  | Type | SER2509□□□MAB |

- Product Description

  - 25.8×19.50mm Max. (L×W), 9.50mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance Range :1.0～68uH.

  - Saturation Current range: 20.0～45.0A .

  - Temperature rise current range 15～40.0A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Mn-Zn core used, Flat wire used.

  - Ideally used in Power module DC-DC Converter

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                             ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| SER2509 | 1.0~68 | 100KHz | 1.00~28.0 | 45.0~20 | 40.0~15.0 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 90% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | SMD power inductors |
| --- | --- | --- |
|  | Type | SER3009□□□MAB |

- Product Description

  - 31.0×21.0mm Max. (L×W), 10.5mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance Range :1.0～68uH.

  - Saturation Current range: 20.0～50A .

  - Temperature rise current range 18～45.0A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Mn-Zn core used, Flat wire used.

  - Ideally used in Power module DC-DC Converter

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                             ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| SER3009 | 1.0~68 | 100KHz | 1.00~25.0 | 50.0~20 | 45.0~18.0 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 90% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | SMD power inductors |
| --- | --- | --- |
|  | Type | SPQ2009□□□MAB |

- Product Description

  - 21.0×15.0mm Max. (L×W), 10.0mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance Range :1.0～100uH.

  - Saturation Current range: 15.0～50A .

  - Temperature rise current range 12～45.0A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Mn-Zn core used, Flat wire used.

  - Ideally used in Power module DC-DC Converter

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                             ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| SPQ2009 | 1.0~100 | 100KHz | 2.00~26.8 | 50.0~15 | 45.0~12.0 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 90% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | power inductors |
| --- | --- | --- |
|  | Type | HPE0909100 MAB |

- Product Description

  - 9.50×7.50mm Max. (L×W), 10.0mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance:10uH.

  - Saturation Current: 6A .

  - Temperature ascending current: 4.70A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Digital Amplifier Inductor/The Flat Wire Use Ferrite Core Type.

  - By using the flat wire, Power inductors can be usrd for large

current with low profile and low resistance.

  - Good shielding, low radiation interference and high fidelity sound effects.

  - Frequency Range: 1MHz

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                             ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| HPE0909 | 10 | 1KHz | 18 Max | 6.0 | 4.70 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 75% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | power inductors |
| --- | --- | --- |
|  | Type | HPE1315□□□MAB |

- Product Description

  - 13.5×8.50mm Max. (L×W), 15.0mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance:10uH、15uH、22uH、27uH、33uH.

  - Saturation Current range: 3.40～6.0A .

  - Temperature rise current range:5.3～8.0A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Digital Amplifier Inductor/The Flat Wire Use Ferrite Core Type.

  - By using the flat wire, Power inductors can be usrd for large

current with low profile and low resistance.

  - Good shielding, low radiation interference and high fidelity sound effects.

  - Frequency Range: 1MHz

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                             ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| HPE1315 | 10~33 | 1KHz | 5.4~14.7 | 6~3.4 | 5~5.3 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 75% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | power inductors |
| --- | --- | --- |
|  | Type | HPE1315100MBB |

- Product Description

  - 13.5×6.50mm Max. (L×W), 15.0mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance:10uH.

  - Saturation Current: 9.0A .

  - Temperature ascending current: 6.0A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Digital Amplifier Inductor/The Flat Wire Use Ferrite Core Type.

  - By using the flat wire, Power inductors can be usrd for large

current with low profile and low resistance.

  - Good shielding, low radiation interference and high fidelity sound effects.

  - Frequency Range: 1MHz

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                             ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| HPE1315 | 10 | 1KHz | 8.8 Max | 9.0 | 6.0 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 75% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | power inductors |
| --- | --- | --- |
|  | Type | HPE1415□□□MAB |

- Product Description

  - 14.5×9.60mm Max. (L×W), 16.0mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance: 10uH、15 uH（W=4.4mm）、22uH（W=5.3mm）、27uH、33uH（W=4.4mm）.

  - Saturation Current range: 3.40～6.0A .

  - Temperature rise current range:5.3～8.0A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Digital Amplifier Inductor/The Flat Wire Use Ferrite Core Type.

  - By using the flat wire, Power inductors can be usrd for large

current with low profile and low resistance.

  - Good shielding, low radiation interference and high fidelity sound effects.

  - Frequency Range: 1MHz

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                             ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| HPE1415 | 10~33 | 1KHz | 5.9~17.5 | 8.3~6.1 | 7.8~5.1 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 75% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | power inductors |
| --- | --- | --- |
|  | Type | HPE1415100MBB |

- Product Description

  - 14.5×7.60mm Max. (L×W), 16.0mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance:10uH.

  - Saturation Current range: 13.5A .

  - Temperature rise current range:6.2A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Digital Amplifier Inductor/The Flat Wire Use Ferrite Core Type.

  - By using the flat wire, Power inductors can be usrd for large

current with low profile and low resistance.

  - Good shielding, low radiation interference and high fidelity sound effects.

  - Frequency Range: 1MHz

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                             ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| HPE1415 | 10 | 1KHz | 12.3 | 13.5 | 6.20 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 75% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | power inductors |
| --- | --- | --- |
|  | Type | HPE1718□□□MAB |

- Product Description

  - 18.0×15.5mm Max. (L×W), 19.3mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance:10uH、22uH、33uH.

  - Saturation Current range: 7.5~26A .

  - Temperature rise current range:8.2A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Digital Amplifier Inductor/The Flat Wire Use Ferrite Core Type.

  - By using the flat wire, Power inductors can be usrd for large

current with low profile and low resistance.

  - Good shielding, low radiation interference and high fidelity sound effects.

  - Frequency Range: 1MHz

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                             ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| HPE1718 | 10~33 | 1KHz | 10.7 | 26~7.5 | 8.20 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 75% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | power inductors |
| --- | --- | --- |
|  | Type | HPE2322□□□MAB |

- Product Description

  - 24.0×21.0mm Max. (L×W), 23mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance:10uH、22uH、33uH.

  - Saturation Current range: 10.4~37.8A .

  - Temperature rise current range:9.4A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Digital Amplifier Inductor/The Flat Wire Use Ferrite Core Type.

  - By using the flat wire, Power inductors can be usrd for large

current with low profile and low resistance.

  - Good shielding, low radiation interference and high fidelity sound effects.

  - Frequency Range: 1MHz

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                             ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| HPE2322 | 10~33 | 1KHz | 9.60 | 37.8~10.4 | 9.40 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 75% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | power inductors |
| --- | --- | --- |
|  | Type | HPE3132□□□MAB |

- Product Description

  - 31.5×19.5mm Max. (L×W), 33mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance:18uH、22uH.

  - Saturation Current range: 30~34A .

  - Temperature rise current range:12.6A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Digital Amplifier Inductor/The Flat Wire Use Ferrite Core Type.

  - By using the flat wire, Power inductors can be usrd for large

current with low profile and low resistance.

  - Good shielding, low radiation interference and high fidelity sound effects.

  - Frequency Range: 1MHz

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                             ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| HPE3132 | 18~22 | 1KHz | 6.3 | 34~30 | 12.6 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 75% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | power inductors |
| --- | --- | --- |
|  | Type | HPQ2622□□□MAB |

- Product Description

  - 27.0×12.5mm Max. (L×W), 23mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance:18uH、22uH.

  - Saturation Current range: 30~34A .

  - Temperature rise current range:12.6A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Mn-Zn core used, Flat wire used.

  - Ideally used in Power module DC-DC Converter

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                             ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| HPQ2622 | 1.0~100 | 100KHz | 2.00~26.8 | 50.0~15 | 45.0~12.0 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 90% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

|  | Product type | power inductors |
| --- | --- | --- |
|  | Type | HPQ3226□□□MAB |

- Product Description

  - 34.5×34.5mm Max. (L×W), 27.0mm Max. height

  - Standard Type, High Power Type, Ultra Power Type are available.

  - Inductance Range :1.0～50uH.

  - Saturation Current range: 30～120A .

  - Temperature rise current range 23～88A.

  - In addition to the standards versions shown here, custom inductors

are also available tomeet your exact requirements.

- Feature& Application

  - Mn-Zn core used, Flat wire used.

  - Ideally used in Power module DC-DC Converter

  - RoHS Compliance and Halogen free.

- Dimensions (mm)

- Pad  Layout(mm)                             ◆ Schematics (Bottom)

- Characteristic description

| TAPE | INDUCTORS (uH) | Test Frequency | DCR (mΩ) | Saturation Current(A) | Temperature Rise Current(A) | Test environment |
| --- | --- | --- | --- | --- | --- | --- |
| HPE3132 | 1.0~50 | 100KHz | 0.60~10.8 | 120.0~30 | 88~23 | 20℃ |

a、Saturation Current: The DC current at which the inductance decreases to 90% of

it's nominal value.

b、Temperature rise current:The DC current at which the temperature rise is

△t＝40℃.(Ta＝20℃)

深圳市品和科技有限公司

深圳龙华三联阁下工业区5栋2楼

陈先生：188 2523 1898

QQ: 898 405 360

# Text boxes

w